钨合金医疗屏蔽件

Tungsten Medical Radiation Shielding

广西晨天钨合金有限公司生产的钨合金屏蔽件，可用于放射源容器，γ射线和X射线的屏蔽件等。钨合金屏蔽件可作为准直器和屏蔽件用于放疗中，也可作为注射器屏蔽件。广西晨天钨合金有限公司生产的钨合金屏蔽件符合以下标准。另外，我们也可根据不同的产品特性，设计和生产特殊规格的钨合金屏蔽件。

Guangxi Chentian Tungsten Alloy Co., Led could offer tungsten alloy radiation shield, which is used for radioactive source containers, gamma radiography, X-ray shields and industrial instrumentation. Tungsten shielding is also serving as collimators and radiation shielding in cancer therapy, as well as syringe protection for radioactive injections. We usually offer tungsten alloy radiation shielding as per the following standard. Besides, we could also design and make special size based on different properties:

| 牌号 Grade | 用途 Application |
| --- | --- |
| HA170 | HA170的延展性最好，最易加工。主要用途包括航空航天领域里的平衡配重件，曲轴，赛车，铆钉顶棒以及辐射屏蔽件。 HA170 is the most ductile and readily machinable grade. Common application areas include counterbalancing weights for the aviation and aerospace industries, crankshaft and auto racing car, bucking bars for rivet setting, and radiation shielding. |
| HA175 | HA175主要用于镗杆，防震工具架和屏蔽件。 HA175 is commonly used to produce chatter-resistant boring bars and tool shanks as well as radiation shielding components. |
| HA180 | HA180 通常是作为配重件使用。它可用于那些需要用到体积小，比重大的配重件的领域。其他用途包括辐射屏蔽件件以及X射线和γ射线的准直器。 HA180 is often applied where size is a factor in the placement of balance or ballast weights. It should be typically of parts with small volume but heavy density. Other applications include radiation shields and collimators of x-ray or gamma ray beams. |
| HA185 | W-Ni-Fe合金中密度最高的一种合金。是医学影像中的屏蔽件的最佳原材料。 The densest of the Ni-Fe binder alloys with tungsten, and is the preferred grade for radiation shielding in the medical imaging industry. |
| HA170C | 成分中的铁被铜所取代，主要作为无磁性部件使用，可作为无磁性的辐射屏蔽件。 Adding copper as a substitute for iron in the binder phase, as there is requirement for nonmagnetic working environment and ideal choice for nonmagnetic radiation shielding. |
| HA180C | 密度比HA170C高，可作为无磁性的大型辐射屏蔽件使用。 Much denser than HA170C, can be used in large scale shielding in nonmagnetic working environment. |

钨合金工业屏蔽件

Tungsten Industrial Radiation Shielding

钨合金屏蔽件可作为核研究中的准直器（用于引导和聚焦射线束）和放射性同位素容器。核研究利用核反应堆和回旋加速器进行放射性材料的研发。钨合金是辐射屏蔽件的最佳原材料，钨合金屏蔽件可屏蔽X射线和γ射线。钨合金的密度比铅高60%，可减小屏蔽件的体积而不影响屏蔽性。

Tungsten shielding is used in research activities as collimators (devices which guide or focus beams of radiation) or containers for radioactive isotopes. Nuclear research use nuclear reactors or cyclotrons to study or create radioactive materials. Tungsten alloy radiation shielding is ideal for radiation protection for both X-ray and Gamma-ray. High density of it is more than 60% denser than lead, which allows a reduction in the physical size of shielding components without compromising its shielding ability.

钨合金屏蔽件的主要用途：

Tungsten alloy radiation shielding is usually used in the following applications:

非破坏性试验钨合金屏蔽件

Non Destructive Testing (NDT) tungsten radiation shielding

非破坏性试验是利用电磁辐射，声音以及材料固有的属性对样品进行检测，包括用显微镜对样品的外表面进行详细地检测。样品的表面要进行抛光处理，样品的厚度需达到电子透视所需的厚度，但样品的制备工艺，光学显微术以及电子显微术还是具有破坏性。而样品的内部只能利用穿透性电磁辐射进行检测，例如X射线和3D X射线。钨合金屏蔽件可屏蔽有害辐射。

NDT methods may rely upon use of electromagnetic radiation, sound, and inherent properties of materials to examine samples, which includes some kinds of microscopy to examine external surfaces in detail. Although sample preparation techniques for metallographic, optical microscopy and electron microscopy are generally destructive as the surfaces must be made smooth through polishing or the sample must be electron transparent in thickness. The inside of a sample can be examined with penetrating electromagnetic radiation, such as X-rays or 3D X-rays for volumetric inspection. Tungsten alloy radiation shielding could be used for radiation protection from the harm radiation.

地质钻井

Geological well logging

地质钻井技术广泛用于石油以及天然气工业领域，包括电缆钻井和钻孔钻井。γ源放入钻孔中，射线就可穿透岩层。所获得的数据可用于分析岩层中是否存在石油或者天然气。钨合金可作为放射源的屏蔽件以及γ射线的准直器。

Geological well drilling is an exploration technique used mainly in the oil and gas industries. It is also known as cable logging and borehole logging. A gamma ray source is lowered into a borehole and the radiation penetrates the rock strata. This data can then be analyzed to determine whether deposits of gas or oil are present. Tungsten alloy is used as shield the radioactive source and to act as a collimator for the gamma beam.

管线检查

Pipe-line inspection

射线可用于检查管线上的焊接点以此来检测管线是否存在裂缝。γ放射源被放置在一辆远程遥控的小车上（有时也会被称之为"猪"），小车就会进入管线中。钨合金准直器可引导射线射向目标。放射源则放置在钨合金屏蔽件内。

Radiation is used to inspect welds and detect cracks in pipelines. A gamma source is mounted on a remote-controlled wheeled trolley (sometimes called a "pig") and travels inside the length of the pipe. A tungsten collimator is used to direct the radiation onto the target, whilst the radioactive source is housed inside tungsten shielding.

为什么要使用钨合金屏蔽件？

Why Use Tungsten Alloy Radiation Shielding?

进行屏蔽设计时，可根据要求屏蔽层达到的总的减弱倍数计算屏蔽材料的厚度.

公式：K = e0.693 d / △1/2

K：屏蔽层的总减弱倍数

△	1/2：该屏蔽材料的半值层值

d：屏蔽层厚度，其单位同半值层厚度，需要将半值层的质量厚度换算成材料的厚度时，再除以材料的密度即可得到。因此，钨合金屏蔽件与其他屏蔽材料例如铅或者Al203相比，屏蔽性相当，而厚度更薄。

When designing tungsten radiation shielding, it will be calculated according to thickness of shielding material to get total weakened multiple for layers of shield.

Formula: K = e0.693 d / △1/2

K: Shield weakened multiple

△ 1/2: The tungsten nuclear radiation shielding material of the half-value layer values

d: Shielding thickness, with the half-value layer thickness of their units, you need to half-value layer thickness of the quality of translation into the thickness of the material, divided by the density of the material can be obtained. In this way, tungsten alloy radiation shielding could be much thinner to have the same protection ability compared with other material such as lead or Al2O3.

3.1高比重钨合金屏蔽件

Tungsten Heavy Alloy Radiation Shielding

为什么需要高比重钨合金屏蔽件

Why Do We Need Tungsten Alloy Radiation Shielding?

随着医疗技术的发展，越来越多的辐射设备出现在我们的生活中。医疗设备和核电站的普及对我们的生活产生了重大的影响。放射线的危害性以及如何保护人们免遭辐射的危害引起了人们的高度关注。因此，对放射线的屏蔽十分必要，例如X射线，γ射线（高能电磁辐射），α粒子（氦原子），β粒子（电子）和宇宙射线等。

With rapid development of medical science, more and more radiation instruments are used in our lives. Medical instruments x-ray and nuclear power stations have become widespread and are now affecting all our lives. It is essential that people paid more attention to radiation and even more important for the institutions to protect public from the radiation exposure and to make sure to protect every radiation source of X-ray radiation, gamma radiation (energetic electromagnetic radiation), radiation of alpha particles (helium atoms) beta particles (electrons) and cosmic radiation, etc.

为了保护病人，医生，护士以及其他人免遭辐射的危害，放射源必须隔离并将其屏蔽。必须将放射性材料的放射性控制在足够低的放射水平下，以免产生有害的电离辐射，这样就不会导致肺癌，皮肤癌等癌症。铅和铁是传统的辐射屏蔽材料，但毫无疑问，高比重钨合金屏蔽件是最佳的选择。之所以选择高比重钨合金屏蔽件作为屏蔽材料，是因为钨合金具有优良的射线吸收能力，高密度性（密度比铅高两倍）以及良好的耐腐蚀性。

In order to protect patients, doctors, nurses and other people who may be exposed to radiation, sources of the radiation must be safely separated and shielded. It is crucial that holding and delivery instruments for radioactive materials would keep the radiation levels low enough, not to create harmful effects of ionizing radiation such as breast cancer, skin cancer, etc. Lead and steel are the traditional protection materials, but tungsten alloy radiation shielding is no doubt the best solution. Excellent radiation-absorption, twice the density of lead and good physical resistance is main reasons to use tungsten alloy radiation shielding.

高比重钨合金屏蔽件的优点

Advantage of Tungsten Alloy Radiation Shielding

科学家发现使用屏蔽件可降低辐射水平,高比重钨合金屏蔽件材料的辐射屏蔽性与材料的密度密切相关。更高的密度意味着更好的射线吸收能力和射线屏蔽能力。由于钨合金的密度比其他材料高，高比重钨合金屏蔽件对射线的吸收能力和屏蔽能力与其他传统屏蔽材料，比如铅更好。高比重钨合金屏蔽件对γ射线有着更好的屏蔽性，从而可减小屏蔽件的体积。和铅相比，相同体积的高比重钨合金屏蔽件拥有更好的射线屏蔽性。

Experts find that radiation exposure could be reduced by maxing shielding. The density of Tungsten Alloy Radiation Shielding material is related to its radiation stopping ability. Higher density means better stopping and absorbing radiation ray . Due to a higher density than most other materials, tungsten radiation shielding has a much higher ability of absorbing and stopping almost rays than others metals such as the traditional radiation shielding - lead. Tungsten radiation shielding greater linear attenuation of gamma radiations means that less is required for equal shielding. Alternatively equal amounts of tungsten shielding provide diminished exposure risks than equivalent lead

由于钨合金结合了高密度性（密度比铅高60%），机械加工性，良好的耐腐蚀性以及高辐射吸收能力（优于铅和钢），高强度，钨合金是屏蔽件的最佳原材料。缩小屏蔽件以及容器的体积和厚度，钨合金屏蔽件依然拥有和铅相同的辐射屏蔽能力。此外，由于钨合金无毒无污染，相比铅和贫化铀，高比重钨合金更环保。

Tungsten heavy alloy is the right material for radiation protection, as its combination of radiographic density (more than 60% denser than lead), machinability, good corrosion resistance, high radiation absorption (superior to lead and steel), simplified life cycle and high strength. Tungsten radiation shielding can provide the same degree of protection as lead whilst significantly reducing the overall volume and thickness of shields and containers. Besides, compared with lead or depleted uranium (DU), tungsten radiation shielding is more friendship for the environments both lead and DU for it is no any toxic.

高比重钨合金的用途

Applications of Tungsten Radiation Shielding

高比重钨合金屏蔽件的使用不受NRC,EPA以及特殊的OSHA条例的约束。所以高比重钨合金屏蔽件作为准直器，放射性同位素容器，放疗放射源容器等，广泛用于核医疗领域。

The usage of tungsten heavy alloy in radiation protection is not subject to NRC, EPA, or special OSHA regulations, so it has been widely used in nuclear medicine as collimator, isotope container, cancer treatment source holder, etc.

放射源容器

Radioactive source containers

γ射线高比重钨合金屏蔽件

Gamma radiography tungsten alloy radiation shielding

钨合金屏蔽块

Tungsten alloy radiation shielding block

石油钻井用的放射源钨合金容器

Tungsten alloy radiation shielding source holders for oil well logging

钨合金X射线准直器

Tungsten heavy alloy X-ray collimators

钨合金PET注射器屏蔽件

Tungsten alloy PET syringe shield

放疗设备屏蔽件

Shielding in cancer therapy machines

放射性注射器屏蔽件

Syringe protection for radioactive injections

钨合金注射器屏蔽件

Tungsten heavy alloy syringe shielding

屏蔽墙

Nuclear shielding wall

钨合金FDG容器

Tungsten Alloy FDG container

焊缝检测

Tungsten heavy alloy inspect welds

核试验设备

Nuclear testing equipment

射线屏蔽桶

Radiation shielding barrel

放射性同位素的生产、运输和储存

Isotope production, transport, and containment

大型放射物存放容器检测设备

Large container inspection devices

放射性同为速同位素容器和加速器

Oncology Isotopic and accelerator based platforms

管道γ射线检测设备

Pipe-line inspection Gamma

核潜艇动力装置屏蔽件

Defense for nuclear submarines

3.2 高比重钨合金屏蔽件产品类型

Product types of tungsten heavy alloy shielding

由于高比重钨合金的高密度、高硬度及超强的防辐射能力，钨合金产品是用来做屏蔽件的最佳材料， 且易加工无毒，本公司提供的高比重钨合金屏蔽件产品主要有：

Due to its high density, high hardness and excellent radioactive protection ability, tungsten heavy alloy is the best material for radiation shielding, and its machining process is non-toxic, products type of tungsten heavy alloy shielding we provide mainly include:

放射性源盛放器

Radioactive source containers

钨合金防辐射罩

Tungsten Alloy Radiation Cover

钨合金防辐射盖

Tungsten Alloy Radiation cap

钨合金防辐射房

Tungsten Alloy Radiation housing

钨合金医疗屏蔽件

Tungsten Medical Radiation Shielding

钨合金X射线靶材 & 钨合金准直器

Tungsten Alloy X-ray Target & Tungsten Alloy Collimator

钨合金多叶准直器

Tungsten Alloy Multi Leaf Collimator

钨合金手机屏蔽件

Tungsten Alloy Mobile Radiation Shielding

钨合金等离子加速屏蔽件

Tungsten Alloy Plasma Accelerator Shielding

钨合金工业用屏蔽件

Tungsten Radiation Shielding in Industry

无铅屏蔽砖

Lead Free Radiation Brick

iPad钨合金屏蔽防护

iPad Tungsten Alloy Radiation Protection

钨合金CT机屏蔽件

Tungsten Alloy Radiation CT Target

钨合金屏蔽聚能环

Tungsten Alloy Radiation Focusing Ring

钨合金屏蔽屋

Tungsten Alloy Radiation Room

钨合金屏蔽壳

Tungsten Alloy Radiation Shell

钨合金屏蔽门

Tungsten Alloy Radiation Shielding Door

钨合金屏蔽保护壳

Tungsten Alloy Cover Shielding Radiation

伽马辐射屏蔽

Gamma radiography shields

钨合金屏蔽薄板

Tungsten Alloy Shielding Sheet

钨合金屏蔽盾

Tungsten Alloy Shielding Tube

钨合金屏蔽箔

Tungsten Film

钨合金屏蔽毯

Tungsten Shielding Blanket

钨合金X射线防护围裙

Tungsten X-ray Protection Apron

钨合金屏蔽漏斗

Tungsten Funnel Shielding

钨合金辐射保护瓶

Tungsten Alloy Vial Shield

钨合金短距离放射治疗屏蔽件

Tungsten Alloy Brachytherapy Shielding

屏蔽块

Shielding block

石油钻井设备

Drilling equipments of oil well

X射线瞄准仪

X-ray collimators

钨合金PET 屏蔽件

Tungsten alloy PET syringe shield

癌症治疗设备屏蔽

Shielding in cancer therapy machines

防辐射注射器保护

Syringe protection for radioactive injections

核屏蔽墙

Nuclear shielding wall

PET 注射器

PET syringe shield

钨制FDG 转移盘

Tungsten FDG transport container

瞄准仪

Collimator for gamma camera

锝发生器

Technetium generator

钨合金辐射源盾

Tungsten Generator Shields

我们也能按照客户要求定制各种钨合金屏蔽件。

We also can provide tungsten alloy shielding as per requirement of customers.

Contact:

Name: KJ GAO

Tel:	86-772-6811029/6811059

Fax: 86-772-6811659

Cell: 8613215340999

E-mail:kjgao@guangxitungsten.com

Web:  www.guangxitungsten.com

Company: Guangxi Chentian Tungsten Alloy Co., Ltd.

Address: Luzhai County Industrial Park, Liuzhou - 545600, Guangxi, China